## Slide 1: Dislocation-Interface Interactions in Silicon
August 10th, 2011 3PM
Lucas Hale
Post Doc
Sandia National Laboratories, CA
Jonathan Zimmerman, Xiaowang Zhou, Neville Moody
Sandia National Laboratories, CA
William Gerberich, Roberto Ballarini
University of Minnesota
Sandia National Laboratories is a multi-program laboratory managed and operated by Sandia Corporation, a wholly owned subsidiary of Lockheed Martin Corporation, for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-AC04-94AL85000.
Funding: NSF NIRT, NSF CMS, AOARD Air Force, Hysitron Inc., ADMIRE

## Slide 2: Super Hard Silicon Nanoparticles
Compressed Si nanoparticles harder than bulk silicon
W.W. Gerberich, et. al, Int. J. of Plasticity 21 (2005) 2391
W.W. Gerberich, et al. Journal of the Mechanics and Physics of Solids 51 (2003) 979.

## Slide 3: Increasing Number of Dislocations
Hardening at low strain with increasing dislocations
Softening at high strains – dislocations reach surfaces

## Slide 4: Simulation Design
Perfect edge dislocations
Systems of 37920, 85648, 152640, and 238784 atoms used
Stillinger-Weber silicon
Two testing methods
  All atoms unconstrained
  Rigid y boundaries

## Slide 5: Dislocation Interaction Simulations
Can mechanically realistic Si-SiO2 systems be easily simulated?
Will dislocation interactions in MD match elasticity based models?
Will oxide retain dislocations for hardness increase?

## Slide 6: Si/SiO2 Potential
Watanabe et al.[1] modification of the Stillinger-Weber is able to model both Si and SiO2
Introduces bond softening function to 2-body term based on Si-O binding energy with coordination
Cutoffs and preferred bond angles less restricted in three-body term
Stable and correct polymorphs
[1] T Watanabe, H Fujiwara, H Noguchi, T Hoshino, and I Ohdomari, Jpn. J. Appl. Phys. 38 (1999) L366

## Slide 7: LAMMPS Implementation
Stillinger-Weber code modified
2 parameter sets in literature, both included
~2X slower than Stillinger-Weber (coordination dependent)
Tested values consistent with report
  Si behaves exactly like Stillinger-Weber
  Si-O dimer energy and bond length
  α-Quartz lattice energy and Si-O length

## Slide 8: Oxide Growth
Use growth routine by Dalla Torre, et al.[1]
Add O atoms at surface
Run LAMMPS
Add new O atoms in leap-frog method
Repeat 2 and 3 until desired thickness
[1] J. Dalla Torre, J.-L. Bocquet, Y. Limoge, J.-P. Crocombette, E. Adam, G. Martin, T. Baron, P. Rivallin, and P. Mur, J. Appl. Phys. 92 (2002) 1084

## Slide 9: Free Surface: No Shear Applied

## Slide 10: Attraction to Interface
Incremental straining with holds
Attraction during last straining
C is 1/4 -1/5 free surface value

## Slide 11: Long Range Repulsion
Dislocation positions remain fixed in unconstrained systems
No dislocation-dislocation repulsion seen
Oxide is repulsive

## Slide 12: Stress State
Oxide places surfaces in tension
Stress gradient results in shear stresses
Long range repulsion

## Slide 13: Summary/Conclusions
Watanabe, et. al Si-SiO2 implemented in LAMMPS
Free surface and short range oxide attraction consistent with dislocation theory
Presence of oxide is repulsive at long range due to stress state of system
Repulsion can lead to dislocation buildup depending on stress state due to oxide